Supplementary information

Quantifying respiratory tract deposition of airborne graphene nanoplatelets: The impact of plate-like shape and folded structure

Hanchao Gao1,2,3, Tobias Hammer2,3,, Xiaole Zhang2,3, Weidong He2,3, Guangbiao Xu‍1* and Jing Wang2,3*

1 Key Laboratory of Textile Science & Technology, Ministry of Education, College of Textiles, Donghua University, No. 2999 North Renmin Road, Songjiang, Shanghai 201620, China

2 Institute of Environmental Engineering, ETH Zurich, 8093 Zurich, Switzerland

3 Advanced Analytical Technologies, Empa, Ueberlandstrasse 129, 8600 Dübendorf, Switzerland

*Corresponding authors

E-mail address: guangbiao_xu@dhu.edu.cn (G. Xu)

jing.wang@ifu.baug.ethz.ch (J. Wang)

Fig. S1 The thickness of airborne GNPs measured from SEM images and well fitted by the normal distribution.

Fig. S2 (a-b) SEM images of airborne GNPs (the folded GNPs were picked out manually and highlighted in yellow circles), (c) geometric diameter distribution of airborne GNPs measured from (a) and (b), (d) the relationship between folding frequency and GNPs geometric diameter.

Fig. S3 Comparison of GNPs aerodynamic diameter between analytical expression derivation and APS measurement.

Fig. S4 Comparison of the drag force among planar GNPs, 60º folded GNPs, 120º folded GNPs, and totally folded GNPs.

Fig. S5 Comparison of spherical particles respiratory deposition between human and different animals (rat, pig and rabbit), (a) total deposition, (b) head airway deposition, (c) TB deposition, (d) alveolar deposition.

Fig. S6 Mesh of the calculation domain. (a) grading mesh of the whole domain generated using blockMesh tool, (b) enlarged mesh for the region near the particle, (c) enlarged mesh for the additional thin layers on the surface.

Fig. S7 Comparison between the CFD results with the Stokes’ law for spherical particles.

Table S1. The folding frequency of GNPs with different geometric diameters

| GNPs geometric diameter (μm) | Number of folded GNPs | Number of uncertain GNPs |  | Number of total GNPs | Folding frequency |
| --- | --- | --- | --- | --- | --- |
| 0 – 1 | 12 | 5 | 84 |  | 0.143 ± 0.030 |
| 1 – 2 | 32 | 8 | 131 |  | 0.244 ± 0.031 |
| 2 – 3 | 17 | 4 | 62 |  | 0.274 ± 0.032 |

Table S2. Numerical simulation results of drag force of folded GNPs with folding angle of 60º and 120º

| Folding angle | Orientation | Diameter (m) | Thick (m) | Velocity (m/s) | Pressure force (N) | Viscous force (N) | Total drag force (N) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 60° | Vertical | 1.40E-06 | 6.60E-08 | 0.00001 | 5.21E-16 | 4.97E-16 | 1.01776E-15 |
|  |  | 1.40E-06 | 6.60E-08 | 0.0001 | 5.21E-15 | 4.97E-15 | 1.01776E-14 |
|  |  | 1.40E-06 | 6.60E-08 | 0.0005 | 2.60E-14 | 2.49E-14 | 5.08879E-14 |
|  | Parallel | 1.40E-06 | 6.60E-08 | 0.00001 | 8.54933E-17 | 7.53656E-16 | 8.39149E-16 |
|  |  | 1.40E-06 | 6.60E-08 | 0.0001 | 8.54933E-16 | 7.53656E-15 | 8.39149E-15 |
|  |  | 1.40E-06 | 6.60E-08 | 0.0005 | 4.27466E-15 | 3.76828E-14 | 4.19575E-14 |
| 120° | Vertical | 1.40E-06 | 6.60E-08 | 0.00001 | 9.24472E-16 | 3.25787E-16 | 1.25026E-15 |
|  |  | 1.40E-06 | 6.60E-08 | 0.0001 | 9.24471E-15 | 3.25787E-15 | 1.25026E-14 |
|  |  | 1.40E-06 | 6.60E-08 | 0.0005 | 4.62235E-14 | 1.62894E-14 | 6.25129E-14 |
|  | Parallel | 1.40E-06 | 6.60E-08 | 0.00001 | 8.95946E-17 | 8.37566E-16 | 9.27161E-16 |
|  |  | 1.40E-06 | 6.60E-08 | 0.0001 | 8.95946E-16 | 8.37566E-15 | 9.27161E-15 |
|  |  | 1.40E-06 | 6.60E-08 | 0.0005 | 4.47973E-15 | 4.18783E-14 | 4.63581E-14 |

Table S3. Lung volume and breathing pattern of humans and different kinds of animals in the MPPD model

| Parameter | FRC (ml) | URT (ml) | Breathing frequency (per min) | Tidal volume (ml) |  | Specification |
| --- | --- | --- | --- | --- | --- | --- |
| Human | 3300 | 50 | 12 | 625 | Male |  |
| Rat | 4 | 0.42 | 102 | 2 | 330g rat |  |
| Pig | 999 | 137.5 | 16 | 449 | 27 kg pig |  |
| Rabbit | 43.7 | 7 | 41 | 29 | 2.9 kg rabbit |  |

Table S4. Typical path lung model for human

|  | Generation number | Number of tubes | L (cm) | d (cm) | θ | φ | V (cm3) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Tracheobronchial | 1 | 1 | 10 | 2.01 | 0 | 0 | 31.73 |
|  | 2 | 2 | 4.36 | 1.56 | 33 | 20 | 16.67 |
|  | 3 | 4 | 1.78 | 1.13 | 34 | 31 | 7.14 |
|  | 4 | 8 | 0.965 | 0.827 | 22 | 43 | 4.15 |
|  | 5 | 16 | 0.995 | 0.651 | 20 | 39 | 5.30 |
|  | 6 | 32 | 1.01 | 0.574 | 18 | 39 | 8.36 |
|  | 7 | 64 | 0.890 | 0.435 | 19 | 40 | 8.47 |
|  | 8 | 128 | 0.962 | 0.373 | 22 | 36 | 13.46 |
|  | 9 | 256 | 0.867 | 0.322 | 28 | 39 | 18.07 |
|  | 10 | 512 | 0.667 | 0.257 | 22 | 45 | 17.72 |
|  | 11 | 1024 | 0.556 | 0.198 | 33 | 43 | 17.53 |
|  | 12 | 2048 | 0.446 | 0.156 | 34 | 45 | 17.46 |
|  | 13 | 4096 | 0.359 | 0.118 | 37 | 45 | 16.08 |
|  | 14 | 8192 | 0.275 | 0.092 | 39 | 60 | 14.98 |
|  | 15 | 16384 | 0.212 | 0.073 | 39 | 60 | 14.54 |
|  | 16 | 32768 | 0.168 | 0.060 | 51 | 60 | 15.57 |
| Alveolar region | 17 | 65536 | 0.134 | 0.054 | 45 | 60 | 20.11 |
|  | 18 | 131072 | 0.120 | 0.050 | 45 | 60 | 30.88 |
|  | 19 | 262144 | 0.092 | 0.047 | 45 | 60 | 41.84 |
|  | 20 | 524288 | 0.080 | 0.045 | 45 | 60 | 66.71 |
|  | 21 | 1048576 | 0.070 | 0.044 | 45 | 60 | 111.61 |
|  | 22 | 2097152 | 0.063 | 0.044 | 45 | 60 | 200.89 |
|  | 23 | 4194304 | 0.057 | 0.043 | 45 | 60 | 347.19 |

L is airway segment length, d is segment diameter, θ is bifurcation angle, φ is gravitational angle, and V is volume.

1. Drag force and equivalent diameters of GNPs with folding angles of 60º and 120º

1.1 Drag force of GNPs with folding angles of 60º and 120º

For GNPs with folding angle of 60°, the drag force and particle velocity was fitted into a linear relationship:

FD_folded (60°,   perpendicular)=7.2*10-5dgVfolded 60°,

FD_folded (60°,   parallel)=6.0*10-5dgVfolded 60°.

For GNPs with folding angle of 120°, the drag force was expressed as:

FD_folded (120°,   perpendicular)=8.9*10-5dgVfolded (120°),

FD_folded (120°,   parallel)=6.6*10-5dgVfolded (120°).

where the unit of FD_folded is N, the unit of dg is m, and the unit of Vfolded is m s-1.

1.2 Equivalent diameters of GNPs with folding angles of 60º and 120º

1.2.1 Aerodynamic diameter da

For GNPs with folding angle of 60° and perpendicular orientation, the drag force FD_folded (60°, perpendicular) and particle velocity Vfolded (60°) was fitted into a linear relationship:

FD_folded (60°,   perpendicular)=7.2*10-5dgVfolded (60°)

where the unit of FD_folded is N, the unit of dg is m, and the unit of Vfolded is m s-1.

By equaling the settling velocity of sphere VTS_sphere with that of platelet-shaped particle, the aerodynamic diameter da_folded (60°, perpendicular) of the GNPs with folding angle of 60° and perpendicular orientation was calculated as:

da_folded (60°,   perpendicular)=250020ρpdgtη

Similarly, the aerodynamic diameter da_folded (60°, parallel) at parallel orientation was calculated as:

da_folded (60°,   parallel)=300420ρpdgtη

For GNPs with folding angle of 60° and random orientation,

da_folded (60°)= da_folded (60°,   perpendicular)sin2φ+da_folded (60°,   parallel)cos2φ

with sin2φ = 2/3 and cos2φ = 1/3.

Using the same derivation method, the aerodynamic diameter of GNPs with folding angle of 120° was calculated as:

da_folded (120°,   perpendicular)=202248ρpdgtη

da_folded (120°,   parallel)=271908ρpdgtη

where the unit of da_folded, dg and t is m, and the unit of ρp is kg m-3.

1.2.2 Sedimentation diameter dg

Compared with aerodynamic diameter which standardizes for both shape and density, the sedimentation diameter only took the shape effect into account. Using the similar calculation method, the sedimentation diameter of GNPs with folding angle of 60° was calculated as:

ds_folded (60°,   perpendicular)=250020dgtη

ds_folded (60°,   parallel)=300420dgtη

For GNPs with folding angle of 120°, the sedimentation diameter was calculated as:

ds_folded (120°,   perpendicular)=202248dgtη

ds_folded (120°,   parallel)=271908dgtη

where the unit of ds_folded, dg and t is m.

1.2.3 Mobility diameter dm

The particle reached terminal electrostatic velocity as the electrostatic force balanced the drag force. For GNPs with folding angle of 60° and perpendicular orientation,

VTE_folded (60°,   perpendicular)= neE7.2*10-5dg

By equaling the terminal electrostatic velocity of sphere with that of GNPs, the mobility diameter of GNPs with folding angle of 60° and perpendicular orientation was expressed as:

dm_folded (60°,   perpendicular)=7.2*10-5dg3πη

Similarly, the mobility diameter dm_folded (60°, parallel) at parallel orientation was calculated as:

dm_folded (60°,   parallel)=5.99*10-5dg3πη

Using the same derivation method, the mobility diameter of GNPs with folding angle of 120° was calculated as:

dm_folded (120°,   perpendicular)=8.9*10-5dg3πη

dm_folded (120°,   parallel)=6.62*10-5dg3πη

where the unit of dm_folded, dg is m.